Innovative Utilization of Plastic Waste in Sustainable Construction: Development of Interlocking Plastic Bricks

Meenal Mategoankar(0000-0003-3776-5624)Aman Shah(0009-0001-3430-9829),

Raj Nahar(0009-0001-7144-742X), Shreevas Navalkar(0009-0000-2028-8572), and

Adit Chheda(0009-0005-4945-0912)

NMIMS’MPSTME, Mumbai,India

Aman.shah06@nmims.edu.in

Abstract

The global challenge of plastic waste management and the pressing need for sustainable construction materials have sparked innovative research into the repurposing of plastic waste. This study provides a comprehensive review of current advancements in transforming plastic waste into eco-friendly building materials, with a particular focus on the development of interlocking plastic bricks. These bricks offer a promising solution to the dual challenges of plastic pollution and sustainable construction by providing a structurally robust and environmentally friendly alternative to traditional materials. Our research evaluates the mechanical properties of these interlocking plastic bricks, highlighting an average compressive strength of 26,83 MPa, which underscores their potential for use in various construction applications. Additionally, we explore the economic and environmental benefits of using recycled plastic in construction, including the reduction of landfill waste and the conservation of natural resources. This study aims to serve as a valuable resource for researchers, policymakers, and industry professionals, guiding them towards the implementation of innovative and sustainable construction practices that contribute to environmental conservation and waste reduction.

Keywords: Plastic waste management, Repurposing plastic, Eco-friendly materials, Interlocking bricks, Sustainable construction, Recycled plastic, Waste reduction, Building materials innovation, Structural strength, Environmental conservation

Introduction

In today's world, recycling plastic is increasingly vital for a sustainable future. Recycled plastic products reduce waste and conserve natural resources [1]. Applications of recycled plastic include bottles, bags, furniture, carpets, clothing, and as construction materials in the form of plastic aggregates or fibers, and in melted form for road construction [2-4].

Plastic recycling involves transforming plastic waste into new products, thereby decreasing reliance on landfills, conserving resources, and mitigating environmental impacts such as plastic pollution and greenhouse gas emissions [5-7]. However, recycling rates for plastics are significantly lower compared to materials like aluminium, glass, and paper. By 2015, approximately 6.3 billion tonnes of plastic waste had been generated globally, with only 9% recycled and merely 1% recycled more than once [8,9]. Most of the plastic waste is either incinerated (12%) or ended up in landfills or as environmental pollution (79%).

A key factor contributing to low plastic recycling rates is the weak demand resulting from the inconsistent and often poor properties of recycled materials [10]. Enhancing the quality and usability of recycled plastics by minimizing the mixing of packaging materials and eliminating contaminants can increase the percentage of fully recyclable plastics and, consequently, market demand for these materials.

This study combines traditional waste management strategies with innovative recycling approaches to convert plastic waste into plastic bricks for the construction sector. It compares these plastic bricks to conventional building materials in terms of mechanical characteristics, durability, and environmental impact. Additionally, the economic viability and scalability of manufacturing plastic bricks for broader use in the building industry are examined.

- Materials and Methods

The methodology follows an experimental approach, primarily focused on the creation of a prototype for innovative interlocking plastic bricks, as detailed below. A distinctive metal mold with a significantly higher melting point than the plastic material was designed for shaping these bricks [Fig. 1 and Fig. 2].

Fig 1. Design model for mold of the brick

Fig 2. Sectional views of the mold of the brick

An innovative prototype of interlocking plastic bricks ensuring water impermeability and mold resistance is created [Fig. 3]. The process of making recycled plastic bricks involves several key steps, from collecting and sorting plastic waste to processing and molding the bricks [Fig. 3].

Fig. 3: Flow chart of making of plastic brick

Plastic waste, such as bottles, containers, and packaging materials, is collected from various sources, including recycling centers, households, and industrial sites. The collected plastic waste is sorted to separate different types of plastics and remove contaminants using conveyor belts and sorting machines. The sorted plastic waste is thoroughly cleaned to remove any remaining contaminants, labels, and adhesives using water and detergent. The cleaned plastic is then shredded into smaller pieces using industrial shredders and granulators. The shredded plastic is melted at 150-200°C in a controlled environment using extruders or injection molding machines. Various additives, such as reinforcing agents or colorants, may be added to enhance the properties of the final product. The molten plastic is injected or extruded into molds with the desired brick shape using injection molding or extrusion machines. The molded bricks are allowed to cool and solidify within the molds [Fig. 6].

2.Method adopted for making the brick

#### 2.1 Plastic Collection and Segregation

The initial phase in the production of bricks from waste plastic is critical and involves the collection and segregation of used plastics from various sources, including residential, commercial, and industrial areas. Collaboration with local communities, municipal waste management services, and recycling centers is essential to establish an effective collection system, ensuring a continuous supply of raw materials.

Post-collection, the plastic waste must be meticulously sorted. This classification is necessary as different polymers have distinct characteristics impacting processing and end-use. Suitable plastics for brick production include high-density polyethylene (HDPE), low-density polyethylene (LDPE), and polypropylene (PP). Segregation is typically conducted based on resin identification codes (RIC), standardized symbols indicating polymer types.

Contaminants such as food waste, paper, and metals are removed during segregation, as these can significantly degrade the quality and performance of the final product. Advanced sorting technologies, including automated sorting machines with sophisticated sensors and artificial intelligence, enhance accuracy and efficiency.

Effective collection and segregation ensure a consistent supply of quality raw materials, contributing to the efficiency and sustainability of the brick-making process. This stage also plays a crucial role in addressing the global plastic pollution crisis by diverting plastic waste from landfills and oceans.

Fig 4: Plastic Collection and Segregation

#### 2.2 Cleaning and Shredding

Plastic recycling is a multi-step process that includes crushing the material into smaller pieces and washing it to get rid of impurities and residues. Washing ensures the integrity of the recycled material by removing adhesives, leftover garbage, food waste, and labels. The effectiveness of the recycling system may be greatly impacted by consumer actions at home.

Friction washers, which remove impurities from plastic by applying pressure, heat, and kinetic energy, were one of the many washing techniques employed. One of the most important steps in recycling plastic is shredding or grinding. After being cleaned and sorted, the plastic is sent through machinery to be reduced in size. The categorization and procedures of the shredder determine the different shredding techniques.

Fig 5: Cleaning and Shredding

#### 2.3 Incineration (Heating and Melting)

Incineration process is carried out by heating the shredded plastic to a liquid state, making it suitable for molding into bricks. The incineration process is performed in a controlled manner to enhance safety and efficiency. Uniform heating is essential to prevent thermal degradation, which releases hazardous gases and affects product quality.

Proper temperature control mechanisms and continuous monitoring is done to ensure a consistent supply of high-quality molten plastic for the subsequent molding stage. Appropriate temperature of 150-200°C is maintained to achieve the desired viscosity and flow properties. The melting temperature varies with the type of plastic processed, with HDPE and LDPE typically melting at 120°C to 180°C, and polypropylene at about 160°C to 170°C.

Fig 5: Waste Incinerator [source: https://t.ly/NpUCk]

#### 2.4 Molding

Molten plastic is poured into specially designed molds as shown in Fig.1 and Fig.2, shaping the material into bricks with specific dimensions and configurations. The design of the molds determines the shape, size, and interlocking features of the bricks, which are essential for structural stability and ease of assembly in construction.

The molds are made from high-temperature-resistant materials to withstand high temperatures without deforming or degrading. To prevent air pockets or voids that weaken the bricks, large quantities of molten plastic must be poured into the molds and evenly distributed. Techniques such as vibration or vacuum assistance are used to eliminate air pockets.

Temperature control is critical to prevent premature cooling and solidification of the plastic before the molds are filled. The cooling rate is controlled to avoid internal stresses and warping in the bricks. Once the plastic in the molds is set, the molds are opened, and the bricks are extracted, ready for the cooling phase.

#### 2.5 Cooling

The plastic goes through a regulated cooling process to change from liquid to solid once it is placed into the moulds and allowed to solidify. Defects like shrinkage, warping, or internal tensions in the bricks is avoided with controlled cooling. The type of plastic used, and the thickness of the bricks are two parameters that affect the cooling rate. Effective cooling techniques, such as water or forced air cooling, were applied. To guarantee consistent cooling rates, which avoid differential contraction inside the bricks and resulting internal tensions and flaws, it is crucial to keep an eye on both the mould and the surrounding temperatures. Bricks with uniform characteristics and the appropriate mechanical strength are produced via uniform cooling. The bricks are taken out of the moulds once they have completely cooled, and any bricks that are clearly faulty or defective are separated.

#### 2.6 Quality Check

The quality check phase in producing sustainable plastic bricks involves inspections and tests to ensure conformity to specifications. After cooling, bricks are visually checked for defects, with defective bricks rectified or rejected. Mechanical testing assesses properties like compressive strength and, while interlocking accuracy is evaluated for structural stability. A standardized quality control protocol documents each step, ensuring high performance and reliability. This process enhances the credibility and adoption of sustainable plastic bricks in the construction industry.

Fig 6: Prototype of interlocking brick

The produced bricks are inspected for defects and undergo mechanical testing to assess strength and durability, ensuring they meet the required standards. The bricks are tested according to IS 1077:1992 [12].

The interlocking plastic bricks were subjected to compression tests, similar to those applied to conventional concrete bricks or clay blocks, to evaluate their structural properties.

3.Results and Discussion

The samples of the material [Fig.7] are prepared and tested for compressive strength. The standard dimensions of the bricks are 190 mm x 90 mm x 90 mm, in accordance with IS 1077:1992 [11]. These measurements correspond to the brick's length, breadth, and height. The compressive strength of the samples was found to be 27 MPa, 26 MPa, and 25 MPa, with an average strength of 26,83 MPa.

| Table 1: Results |  |  |
| --- | --- | --- |
| Sample sr.no | Compressive Strength (MPa) | Average Compressive Strength (MPa) |
| 1 | 27 |  |
| 2 | 26 | 26,83 |
| 3 | 25 |  |

| Fig 7. Test samples |  |
| --- | --- |

These plastic bricks can be used for constructing parapet walls or decorative structures. Their colourful appearance adds aesthetic value, and the interlocking design eliminates the need for binding materials.

4.Conclusion

Recycling plastic is a major global challenge, as is the use of sustainable construction materials. This study developed recycled plastic bricks with specified dimensions using a comprehensive methodology encompassing collecting, sorting, cleaning, shredding, melting, and moulding plastic. The process ensures that different types of plastics, such as high-density polyethylene (HDPE), low-density polyethylene (LDPE), and polypropylene (PP), are carefully segregated and processed to achieve optimal quality and performance. The resulting interlocking bricks meet the required standards of strength (25-27 MPa) and mechanical properties, making them suitable for various construction applications. These bricks are not only durable and robust but also aesthetically pleasing, providing an attractive solution for partition walls and potentially other structural components.

The production process emphasizes the importance of uniform heating and cooling to prevent defects such as warping, internal stresses, and voids, thereby ensuring the bricks' structural integrity. Advanced technologies such as automated sorting machines and controlled incineration methods like pyrolysis and gasification are employed to enhance efficiency and minimize environmental impact. Quality checks at each stage of production guarantee that the final product adheres to stringent standards, offering reliable and consistent performance.

This research represents a significant step towards addressing plastic waste challenges and introducing innovative, sustainable interlocking plastic bricks to the construction industry. By diverting plastic waste from landfills and oceans, the study contributes to environmental preservation while promoting the use of eco-friendly building materials. The interlocking feature of these bricks not only facilitates easy assembly and disassembly but also enhances the stability and versatility of construction projects.

Furthermore, the study aligns with and supports the Sustainable Development Goals (SDGs), particularly Goal 9 (Industry, Innovation, and Infrastructure) and Goal 11 (Sustainable Cities and Communities). By fostering industry innovation through the development of new materials and construction techniques, and by

contributing to the creation of sustainable, resilient, and inclusive urban environments, this research paves the way for a more sustainable future. The introduction of recycled plastic bricks could revolutionize the construction industry, reducing reliance on traditional materials, decreasing carbon footprints, and promoting a circular economy.

5.References

[1] Al-Salem, S.M., Lettieri, P., Baeyens, J. (2009). Recycling and recovery routes of plastic solid waste (PSW): A review. Waste Management, 29(10), 2625–2643. doi:10.1016/j.wasman.2009.06.004. PMID 19577459

[2] Puttaraj, M., Shetty, S., Rai, N., T.B. P. (2014). Utilization of Waste Plastic in Manufacturing of Plastic-Soil Bricks. International Journal of Technology Enhancements and Emerging Engineering Research, 2, 102–107.

[3] Shanmugavalli, B., Gowtham, K., Jeba Nalwin, P., Eswara Moorthy, B. (2017). Reuse of Plastic Waste in Paver Blocks. International Journal of Engineering Research, 6(2). doi:10.17577/IJERTV6IS020162

[4] Tapkire, G., Parihar, S., Patil, P., Kumavat, H.R. (2014). Recycled Plastic used in Concrete Paver Block. International Journal of Research in Engineering and Technology, 3(Special Issue: 09), NCETCE-2014. eISSN: 2319-1163

[5] Ignatyev, I.A., Thielemans, W., Vander Beke, B. (2014). Recycling of Polymers: A Review. ChemSusChem, 7(6), 1579–1593. doi:10.1002/cssc.201300898. PMID 24811748

[6] Lazarevic, D., Aoustin, E., Buclet, N., Brandt, N. (2010). Plastic waste management in the context of a European recycling society: Comparing results and uncertainties in a life cycle perspective. Resources, Conservation and Recycling, 55(2), 246–259. doi:10.1016/j.resconrec.2010.09.014

[7] Hopewell, J., Dvorak, R., Kosior, E. (2009). Plastics recycling: challenges and opportunities. Philosophical Transactions of the Royal Society B: Biological Sciences, 364(1526), 2115–2126. doi:10.1098/rstb.2008.0311. PMID 19528059

[8] Lange, J.P. (2021). Managing Plastic Waste─Sorting, Recycling, Disposal, and Product Redesign. ACS Sustainable Chemistry & Engineering, 9(47), 15722–15738. doi:10.1021/acssuschemeng.1c05013

[9] Geyer, R., Jambeck, J.R., Law, K.L. (2017). Production, use, and fate of all plastics ever made. Science Advances, 3(7), e1700782. doi:10.1126/sciadv.1700782. PMID 28776036

[10] European Commission. (2018). A European Strategy for Plastics in a Circular Economy, COM (2018) 28 final.

[11] IS 1077: 1992 Amendment No. 1 (2008). Common Burnt Clay Building Bricks — Specification (Fifth Revision).

.

| Aman A Shah Civil Engineering student, Student at NMIMS’ MPSTME, Mumbai. Aman.shah06@nmims.edu.in Aman Shah, born 2003, will receive his civil engineering degree from the Univ. of NMIMS |  |  | Raj S Nahar Civil Engineering student, Student at NMIMS’ MPSTME, Mumbai. raj.nahar66@nmims..in Raj Nahar, born 2003, will receive his civil engineering degree from the Univ. of NMIMS |  |
| --- | --- | --- | --- | --- |
| Shreevas S Navalkar Civil Engineering student, Student at NMIMS’ MPSTME, Mumbai. shreevas.navalkar34@nmims.in Shreevas Navalkar, born 2003, will receive his civil engineering degree from the Univ. of NMIMS Dr.Meenal Mategaonkar Professor & Head, Department of Civil Engineering, NMIMS’ MPSTME, Mumbai Meenal.mategaonkar@nmims.edu |  | Dr. Meenal Mategaonkar is a renowned researcher and educator, known for her significant contributions to her field. She holds a Ph.D. in her area of expertise, demonstrating a strong commitment to academic excellence. A respected leader and mentor, she has inspired many through her dedication and innovative work. | Adit R Chheda Civil Engineering student, Student at NMIMS’ MPSTME, Mumbai. Adit.chheda69@nmims.in Adit Chheda, born 2003, will receive his civil engineering degree from the Univ. of NMIMS |  |